## Slide 1
未溶融
Koki no-clean LEAD FREE flux cored wire solder
REACH Compliant
72M Series
S3X
S01X7Ca
S03X7Ca
SB6N
LINE-UP
- 72M
- 72M
- 72M
- 72M
Significantly improved wettability results in wider process range
Improved wettability without compromising flux sputtering
Improved wettability to various metals (brass, nickel, etc…)
Helps preventing defects (bridging and insufficient solder feeding), owing to improved surface covering property of flux
Reduced soldering fume for manual soldering

## Slide 2: Flux Cored Wire Solder 72M series
■ Powerful wetting & High reliability S3X-72M (Sn 3.0Ag 0.5Cu)
Need for Soldering robot.
FAST wettiing → FAST “slide” soldering
Required performance
・ Fast removal of oxide film
・ Resistant to heat from solder iron
・ High reliability
Solution
・ Employment of a new activator system that has FAST-acting nature
・ Koki patented technology
 | Bottom | Top
S3X-72M |  | 
従来品 |  | 
High speed slide soldering
Activator B:
Slow acting
Activator A:
Short durability
Wetting
Activator C:
Bridge
Good
Durability

## Slide 3: Flux Cored Wire Solder 72M series
>SIR in HAST
(HAST: 110CO, 85%RH, DC50V applied in IPC-B-24 board)
Excessive volume of activation agent → Deterioration of electrical (SIR/EM) and chemical (corrosion) reliability.
Flux residue from 72M series ensures high reliability even under HAST environment as shown above.
Chart: Competitive product
Chart: S3X-72M
Occurrence of EM
Dendrite growth
No electromigration
(Highly Accelerated temperature and humidity Stress Test) by IEC 68-2-66

## Slide 4: Flux Cored Wire Solder Low Ag 72M series
未溶融
16.8%
50.5%
初期 | S3X (SAC305) | S03X7Ca
■ Anti-erosion technology S03X7Ca-72M (Sn 0.3Ag 0.7Cu 0.03Co + a)
Melted
SAC305
Melted
S03X7Ca
with Co
Sn-Fe
Sn-Co-Fe / Sn-Co
Fe diffusion
Fe diffusion less
Schematic view of reaction between
iron tip and melted solder
After 10000 shots
Iron tip
Cross-section
Fe
Cu
S3X
(Sn 3.0Ag 0.5Cu)
S03X7Ca
(Sn 0.1Ag 0.7Cu 0.03Co + α)
Solder
Solder
Iron tip (Fe)
>EMPA analysis of boundaries between solder and iron tip
Iron tip (Fe)
Barrier layer
通常の反応層
Solder
Iron tip (Fe)
Chart: Number of shot
| 0 | 10000 | 20000 | 30000 | 50000 | 84000 | 100000 | 150000 | 200000 | 250000
S03X7Ca | 0 | 25 | 45 | 85 | 105
SAC305 | 0 | 120 | 230 | 270 | 410
Sn60/Pb | 0 | 40 | 60 | 100 | 140 | 240
 | 470 | 470 | 470 | 470 | 470 | 470 | 470 | 470 | 470 | 470
Iron layer
>4 times longer Iron bit life!

## Slide 5: Flux Cored Wire Solder Low Ag 72M series
■ Joint reliability after repairing
> Solder joint reliability in re-soldering by S03X7Ca
Pull
45deg.
QFP
Repair SAC305 joint with
S03X7Ca-72M
Mixture of alloys
Chart: S03X7Ca content (%) in SAC305
| 0 | 25 | 50 | 75 | 100
0 cyc. | 18.595 | 16.0329 | 17.8841 | 16.7684 | 15.4568
500 cyc. | 17.1607 | 16.597 | 16.9279 | 17.1607 | 15.7633
1000 cyc. | 16.6827 | 15.322 | 18.178 | 17.5406 | 14.4272
> 45 deg. Lead Pull test
T/C: -40/125OC
Result:
Mixture of S03X7Ca in each rate (0~75%) show similar strength.
No deterioration in joint strength even after the T/C occurred.
The results suggest that S03X7Ca ensures equivalent joint reliability as high as SAC305.
Solder joint
QFP (0.65P)
Iron slide direction
Expected combination of SAC305 : S03X7Ca-72M are;
(1) SAC305 = 100
(2) SAC305 : S03X7Ca = 75 : 25
(3) SAC305 : S03X7Ca = 50 : 50
(4) SAC305 : S03X7Ca = 25 : 75
(5) S03X7Ca = 100
T/C condition: -40/125OC x 1000cyc
Measure joint strength
QFP